连续粒度分布简介

Particle size distribution data can be presented numerically (tabular format) or graphically. When presented graphically, there are two types: differential and cumulative. They are related. If one differentiates the cumulative distribution

curve, the differential distribution is obtained. If one integrates the differential distribution curve, the cumulative distribution is obtained.

粒度分布数据可以用数字（表格格式）或图形表示。以图形方式呈现时，有两种类型：微分分布和积分分布（累积分布）。这两种分布是相关的：如果有积分分布曲线，则可以得到微分分布。如果微分分布曲线，则获得积分分布。

Differential Distribution: The differential distribution shows the relative amount* at each size. For example, for the one shown here, using a ruler to draw horizontal and vertical lines, one can determine that the differential amount at 14.5 nm is about 40 while at 18 nm it is about 20. Therefore, the differential distribution is telling us there is twice the amount at 14.5 nm compared to the amount at 18 nm.

微分分布：该分布形式显示每个尺寸的相对数量（或其他权重，如重量或光强）。例如，下图中，使用标尺绘制水平线和垂直线，可以确定14.5 nm处对应微分分布值约为40，而18 nm处的值约为20。因此，通过微分分布可知14.5nm处含量为在18nm处含量的两倍。

Measures of central tendency such as the modal and mean diameters are determined from the differential distribution. The modal diameter is the diameter at the peak of the differential distribution. In this example it is 8.5 nm. The mean diameter is the average diameter. In this example it is 10.7 nm.

中心趋势量，如众数和平均直径也由微分分布确定。众数直径是差分分布峰值处对应的直径。在这个例子中众数直径是8.5nm。平均直径是在当前权重下的平均直径，在这个例子中是10.7nm。

This distribution is unimodal (single peaked) but not monodisperse (all one size). It has a width. There are several measures of width just as there are several measures of central tendency. One measure of width is FWHM, the full width at half maximum. It is obtained by drawing a horizontal line at 50% of the maximum and taking the difference between the two places it intersects

the distribution. In this example it is 8.4 nm.

这种分布是单峰（单峰），但不是单分散（全尺寸）。实际上，它存在一个宽度。正如有几种集中趋势测量方法，同样有几种宽度表征方法。其中较为常用的是FWHM值，即半高宽，它通过在最大值的50％处绘制水平线，并获取它与分布相交的两个位置之间的差异值。在这个例子中FWHM值是8.4nm。
HWHM, the half width at half maximum, is another measure of width. It is defined as FWHM/2. In this example it is 4.2 nm.

HWHM是半高半宽，是宽度的另一种度量。它被定义为FWHM / 2。在这个例子中它是4.2nm。

FWHM and HWHM are measures of absolute width. Both have the same units as the diameter, nanometers in this example. A relative fractional measure of width is obtained by dividing either FWHM or HWHM by the measure of central tendency from which it was derived, the modal diameter. In this example the HWHM/Modal Diameter is 4.2/8.5 = 0.49. A relative percent measure of width is then 49% in this example. Neither measure of relative width has units.

FWHM和HWHM是绝对宽度的度量。在这个例子中，两者单位为纳米。宽度的相对分数测量是通过将FWHM或HWHM除以由其得出的中心趋势测量值（模态直径）获得的。在这个例子中，HWHM /众数直径是4.2 / 8.5 = 0.49。在这个例子中，宽度的相对百分比度量是49％。相对宽度的度量都没有单位。

Given that a differential particle size distribution looks like the distribution of repeated measurements of any quantity, it is not surprising that the mathematics of probability distributions permeate the descriptions used in particle size distributions; namely, average (mean), variance, standard deviation, etc. Unfortunately, variance and standard deviation also suggest error or uncertainty in any measurement. Indeed, there is uncertainty in particle size distribution measurements; however, when the width of the differential size distribution is represented by the standard deviation of that distribution, it is not meant to suggest it represents the error in the measurement. Rather it is another way of representing the width of the size distribution. In fact, with repeated measurements of the size distribution, one could specify the standard deviation (the error) of the distribution’s standard deviation (width of the distribution).

考虑到微分粒度分布看起来像是任何数量的重复测量的分布，数学中概率分布算法通常用于粒度分布的描述：即平均值（均值），方差，标准偏差等。不幸的是，方差和标准偏差也表明测量中的误差或不确定性。事实上，粒度分布测量存在不确定性；然而，当微分尺寸分布的宽度由该分布的标准偏差表示时，并不意味着它表示测量中的误差。相反，它是表示尺寸分布宽度的另一种方式。事实上，通过重复测量尺寸分布，可以指定分布标准偏差（分布宽度）的标准偏差（误差）。

The standard deviation is not shown in the differential distribution above in order to keep the graph readable. If it was, one could define absolute and relative (fractional and percent) standard deviations (dividing by the mean diameter).

上述微分分布中未显示标准偏差以保持图表可读。如果是，可以定义绝对和相对（分数和百分比）标准偏差（除以平均直径）。

The differential distribution shown here is not symmetric about the modal diameter. If it was, and because the diameter axis is linear, then the modal, mean, and median (defined for the cumulative distribution) diameters would all be equal. Such is not the case here. The distribution is skewed to larger sizes. There are various definitions of skew that are derived from probability

distributions. In all cases, the skew is positive when the curve tails to the right more than to the left, and it is negative when the curve tails to the left more than to the right. The reference point for tailing is with respect to the modal diameter. A symmetric differential distribution has zero skew.

此处显示的微分分布关于众数直径并不是对称的。如果此图是对称的，并且由于X-轴是线性坐标，则众数，平均值和中值（对于累积分布定义d50）直径将全部相等。情况并非如此。分布偏向较大的尺寸。从概率分布中可以推出各种各样的倾斜定义：在所有情况下，当曲线向右拖尾时，偏斜Skew是正值，而当曲线向左拖尾时，偏斜Skew是负值，拖尾的参考点是众数直径。当出现对称微分分布时，Skew具有零偏斜。

Cumulative Distribution: The corresponding cumulative distribution is also shown. The cumulative undersize distribution shows the relative amount* at or below a particular size. In this example 50% of the amount of particles is at or below 9.5 nm. Ninety percent are at or below 16.2 nm. These are just two of the possible percentile diameters.

积分分布：一般粒度分布图中，还显示相应的积分分布（累积分布）。积分分布显示相对数量（或其他权重，如重量/体积或光强）等于或低于特定尺寸。在这个例子中，50％的颗粒等于或低于9.5nm。90%的颗粒等于或低于16.2纳米。这只是两种可能使用到的百分比所对应的直径值。

The median diameter is another measure of central tendency. It is the diameter at the 50th percentile, designated d50. Quartile diameters include

d75, d50, and d25. There are several measures of absolute width one can derive given the cumulative distribution. One common measure is the span, d90 –d10. In this example it is 10.7 nm. A dimensionless measure of width is the relative span defined as span/d50. In this example it is 1.13. Other

relative measures of width include percentile ratios such as d90/d10 and d75/d25. In this example these values are 2.95 and 1.77, respectively.

中值直径是集中趋势的另一个度量标准。它是第50百分数对应的直径，指定为d50。四分之一直径包括d75，d50和d25。考虑到累积分布，可以推导出几种绝对宽度的度量。一个常见的措施是跨度，d90 -d10。在这个例子中它是10.7纳米。宽度的无量纲测量是相对跨度，定义为跨度/ d50。在这个例子中它是1.13。宽度的其他相对度量包括百分比例如d90 / d10和d75 / d25。在这个例子中，这些值分别是2.95和1.77。
The narrower a distribution is the more closely the absolute measures of width approach zero: FWHM, HWHM, variance, standard deviation (square root of variance), and span. Whereas, most of the relative measures of width like

d90/d10 and d75/d25 approach unity.

越窄的分布越接近宽度接近零的绝对测量值：FWHM，HWHM，方差，标准偏差（方差的平方根）和跨度。而大部分宽度的相关度量，例如d90 / d10和d75 / d25接近1。

Which Distribution Should I Use To Best Present My Data? It depends on what is customary in your particular field. For example, long ago tire manufactures correlated the relative strength of tire treads and tire walls to the quartile ratio d75/d25. And so to represent the distribution width use this relative width obtained from the cumulative distribution.

应该使用哪种分布以最好地呈现数据？这完全取决于用户所处的特定领域的惯例。例如，以前轮胎制造商将轮胎胎面和胎壁的相对强度，用四分位数比率d75 / d25表示。因此，为了表示分配宽度，请使用从累积分布中获得的相对宽度。
Suppose you are the first in your field, so there are no guidelines. Then you have the golden opportunity to define which statistics work best. Perhaps you determine that the mean must be (5 +/- 1) micron and that 95% must be at or below 20 micron. Thus, d95 must be less than or equal to 20 micron. Therefore, you need to show the differential and the cumulative distributions.

假设用户是行业第一，有可能没有指导原则。那么就有机会定义使用哪些统计数据效果最好。也许你确定平均值必须是（5 +/- 1）微米，95％必须在20微米或以下。因此，d95必须小于或等于20微米。因此，就需要同时显示微分和积分分布。

Although the examples in this paper are for continuous distributions, in the next paper discrete distributions will be examined. Yet, while we are on the subject of how best to present data, the example of a limited number of size classes in a discrete, cumulative distribution is relevant.

虽然本文中的例子是用于连续分布的，但在下一篇论文中将会考察离散分布。然而，尽管我们讨论的是如何更好地呈现数据，但在离散累积分布中有限数量的大小分级的例子也是相关的。
This is the case with sieves where the 4th root of two, 1.189, is the ratio of successive sieve openings. In such a circumstance, while the statistics

derived from the cumulative distribution may be useful, trying to numerically differentiate is difficult, leading to large errors in the statistics derived from the resulting differential distribution. In such a case, stay with the statistics derived from the cumulative distribution: the median, span, and percentile ratios.

筛网的情况就是这样，其中相邻筛孔的比例是2开4次方（1.189）。在这种情况下，从积分分布中得出的统计数据可能有用，但得到微分数值比较困难，从而导致微分分布得出的统计数据中的较大误差。在这种情况下，请保留累积分布的统计数据：中位数，跨度和百分位数比率。

* The amount could be by number, by surface area, by volume, by mass, by intensity of scattered light. The distributions “weighted” by these quantities are all shifted with respect to one another. The topic of weighting is discussed in another entry in this series on particle sizing.